## Slide 1
EXPERIENCES WITH TROPICAL SOIL
DR K BALAN
Geotechnical Engineering Consultant
Former Professor in Civil Engineering
College of Engineering
Trivandrum

## Slide 3
Laterite is a residual material left after in situ weathering of
parent rock under humid tropical conditions.
At least three different basic structural types in Kerala
Laterites with a continuous coherent skeleton, which can be
considered as a vesicular soft rock. The vesicules are usually
Filled with clay. The hardness and extent of vesicules are variable.
Referred as brickstone.
Latertites formed as a result of cementation of pre-existing
Materials like gravels, sands and pebbles by ferruginous matter.
Conglomerate.
3. Hard elements existing as free concretions or nodules
In an earthy matrix. Lateritic gravelly soil.

## Slide 4
Gravelly soil extends to 60 cm
Hard to Medium Laterite extending upto 7 to 10 m
Soft Laterite/Kaolinitic clay
Disintegrated rock
Hard rock

## Slide 5
At places, where laterite is exposed, it is very hard at the surface.
Some types of this hard laterite are very dense and darker in
colour, due to presence of iron.
They are known as Narickallu or Chenkallu
Laterite is met with at considerable depth, say 18 to 27 m
below the ground level (other than the three varieties), at
places like Ernakulam.
This lateritic hardpan is used to support end-bearing piles.

## Slide 6
60 cm diameter pile resting at 8 m blow ground level in Trivandrum with its tip in a layer having SPT 40 can take over 100 tonnes.
SPT varies
For soft laterites 20 to 30
Hard laterites 100
Laterite having N value 30 shows
Angle of internal friction as 35 degrees and
Cohesion about 0.9 kg/cm2.
Average compressive strength of 15 cm cube was
1.79 kg/cm2

## Slide 7
Theoretical Bearing capacity for a 30 cm plate was found
to be 400 t/m2.
Whereas the actual value was found to be 82 t/m2.
Settlement criterion should govern the design.

## Slide 8
In General, the properties can be summarized as follows., though
It varies drastically whether the test is conducted on fresh
Samples or on samples air dried or oven dried.
Properties of the first two varieties
Property | Range of values | Remarks
Bulk density | 1.8 to 2.2 t/m3 | Upto 3.5 t/m3 for surface layers
Natural water content | 5 to 21% | 
Specific Gravity | 2.68 to 2.7 | 
Void ratio | 0.5 to 0.6 | 
Porosity | 36 to 38% | 
Grain size, Gravel | 46 to 59% | 
Sand | 26 to 37 % | 
Silt | 7 to 14% | 
Clay | 4 to 6% | 
% Swelling | Negligible | 

## Slide 9
Property | Range of values | Remarks
Liquid Limit | 39 to 46% | 
Plasticity Index | 9 to 13 % | Sometimes NP
Compressive strength | 4.5 to 6.5 kg/cm2 | On 10 cm cube fresh
 | 9 to 11 kg/cm2 | On some samples
 | 14.5 kg/cm2 | Air dried
 | 19.5 kg/cm2 | Oven dried
Modulus of elasticity | 260kg/cm2 | UCC on 3.8x7.6 cm sample
 | 660 kg/cm2 | 
%Absorption of water | 15 to 23% | 
Triaxial | Φ = 40 and C=0.8 kg/cm2 | 3.8 x 7.6 cm sample. Strain 0.6%

## Slide 14
Bakel Fort

## Slide 17
Aranmula, Pandalam

## Slide 21
Kasargode

## Slide 28
Cutting in Trivandrum

## Slide 31
Cutting at Kollam

## Slide 32
Comparison of cut surface
In laterite at Trivandrum
and Kollam

## Slide 34
Cutting in Kakkanad, Ernakulam

## Slide 42
Cutting at Nemom, Trivandrum, Rail doubling project

## Slide 45
Railway cutting at Parassala

## Slide 50
Kottayam

## Slide 76
Existing House
BH1
BH2A
BH2
BH3
Rain water harvesting
WELL
BH4

## Slide 77
Thank you