## Slide 1: Third Alternative - GRGB
Madhav Madhira
Academic, Researcher & Consultant

## Slide 2: Shallow Foundations
ground
bed rock
firm ground

## Slide 4: Failure Modes

## Slide 5: Deep Foundations
bed rock
weak soil
~ For transferring building loads to underlying ground
~ Mostly for weak soils or heavy loads

## Slide 6: Deep Foundations
Unsuitable
Soil
Bearing Layer
Tip Resistance
Side
Resistance
End Bearing
Friction
Tip Resistance (small)
Q
Q

## Slide 7: The Third Alternative GI/GRGB
Structure Ground | Light | Medium | Heavy
Soft | Shallow Found./G.I | Gr. Impr. (G.I.) | Deep Found.
Medium Stiff | Shallow Found. | Gr. Impr. (G.I.) | Deep Found./ (G.I.)
Hard | Shallow Found. | Shallow Found./G.I. | Shallow Found./G.I

## Slide 8: Foundation Options

## Slide 9
Engineering of Ground
Dynamic compaction
Preloading
Vibro- methods/Stone Columns
Dewatering
Grouting
Micropiling
Reinforced foundation beds

## Slide 10: Commonly Used Geosynthetics
Geotextile (GT)
Geogrid (GG)
Geocell (GC)

## Slide 11: Geogrid & Geocell

## Slide 12
Confinement
Interlocking
Confinement

## Slide 13: Basal reinforcement

## Slide 14: Airport Runway

## Slide 15: Load Transfer on to Piles

## Slide 16: Load Transfer Platform

## Slide 17: High Speed Railway Track

## Slide 18: Sports Field over Landfill

## Slide 19: Mine Tailing Pond Closure

## Slide 20: Sludge Lagoon Closure

## Slide 21: Reinf. Found. Bed for Waste Treatment Plant

## Slide 22: RFB for Industrial Structure

## Slide 23: Borelogs STP

## Slide 25: STP

## Slide 26: GRFB for STP

## Slide 29: Central school complex

## Slide 30: Antenna Foundation

## Slide 35: Krishna University, Machilipatnam

## Slide 36: KU 2

## Slide 37: Soft Ground

## Slide 40: Geocell
Lightweight but strong three dimensional honeycomb-like cellular confinement system
Honeycomb structure - strongest structural systems
Fabricated from ultrasonically-welded HDPE strips that are expandable at site
Confinement of non-cohesive material within provides rigidity
Perforated for porewater pressure relief
Textured within for better soil-cell wall interaction

## Slide 41: applications of Geocell

## Slide 42: Principle of Geocells
Geocells filled with cohesionless material - semi-rigid raft/mat
p

## Slide 43
Geogrid Reinforced Granular Foundations

## Slide 45: PLT with 750 mm dia Plate of GRFB

## Slide 46: PLT with 300 mm square Plate on GRFB

## Slide 47: Plate Load Tests
Chart: Load (kPa)
| 0 | 75.821656050955411 | 151.64331210191082 | 227.46496815286625 | 303.28662420382165 | 379.10828025477707 | 454.9299363057325 | 556.02547770700642 | 631.84713375796173
Non Cyclic - Upto Failure | 0 | 0.65 | 1.76 | 2.56 | 3.22 | 3.94 | 4.72 | 6.12 | 7.57

## Slide 48
Degrees of improvement:
Bearing capacity ratio, BCR = ratio of bearing capacities of reinforced to unreinforced cases
Sub-grade stiffness improvement factor, Ik = ratio of moduli of subgrade reactions of reinforced to unreinforced cases
Settlement reduction factor, SRF = ratio of settlements of reinforced to unreinforced cases at different percentages of normalized settlements

## Slide 49: Bearing Capacity of Found. On Strong Soil over Weak One

## Slide 50: Lateral Confinement, Load Spread & Membrane Mechanisms

## Slide 52
Bearing Capacity of Embedded Circular Footings
on Reinforced Foundation Beds over Soft Compressible Ground

## Slide 54
Chart: D/H
| 0 | 0.4 | 0.60000000000000064 | 0.8 | 1
unreinforced | 1.1 | 0.78 | 0.7 | 0.64 | 0.58
reinfroced | 0.42 | 0.36 | 0.34 | 0.34 | 0.32
Effect of Reinforcement on Critical Granular layer thickness

## Slide 55
Chart: D/H
| 0 | 0.4 | 0.60000000000000064 | 0.8 | 1
63 | 7.7 | 4.48 | 3.8 | 3.33 | 2.87
350 | 6.9 | 4.2 | 3.6 | 3.11 | 2.69
1000 | 6.44 | 4.06 | 3.51 | 3.02 | 2.62
63 for 5 | 2.69 | 1.96 | 1.73 | 1.55 | 1.4
350 for 5 | 2.08 | 1.58 | 1.41 | 1.28 | 1.16
1000 for 5 | 1.83 | 1.4 | 1.26 | 1.14 | 1.04
(BCR)ax* versus D/H- Effect of G/su and γB /su

## Slide 56
Chart: φ in degrees
| 30 | 35 | 40
63 unreinf | 3.84 | 4.77 | 6.74
150 unreinf | 10.06 | 12.77 | 15.77
350 unreinf | 3.25 | 3.91 | 5.27
1000 unreinf | 3.02 | 3.51 | 4.69
63 reinf | 11.82 | 14.68 | 18.34
150 reinf | 10.06 | 12.77 | 15.77
350 reinf | 8.78 | 11.27 | 13.89
1000 reinf | 7.59 | 9.88 | 12.15
(BCR)ug, (BCR)ax versus  - Effect of G/su

## Slide 57
Chart: H/B
Ncg versus H/B- Effect of γB /su and G /su

## Slide 58: Effect of Stiff Layer over Softer One

## Slide 59
Ueshita and Meyerhof (1967)

## Slide 61
Case study 1: (Hegde and Sitharam - 2013)
Homogenous sand bed reinforced with geocell and geogrid underlying square footing

## Slide 66
h/B effect: d/B=1.2; b/B=12; u/B=0.1
h/B | Eeq/E2 | Er/E2
0.8 | 1.23 | 4.16
1.6 | 2.04 | 8.6
2 | 2.12 | 4
2.75 | 2.12 | 2.6
3.14 | 2.16 | 2.38

## Slide 68
b/B effect: d/B=0.8; h/B=1.2; u/B=0
Governing equations:
b/B | Eeq/E2 | Er/E2
1 | 2.12 | 2.98
2 | 2.12 | 2.98
4 | 2.22 | 3.24
6 | 2.27 | 3.27
8 | 2.48 | 4
10 | 2.79 | 5.18
12 | 3 | 6.19

## Slide 69
h/B effect: d/B=0.8; u/B=0; b/B=4.9
h/B | Eeq/E2 | Er/E2
0.6 | 1.63 | 4.28
1.2 | 2.1 | 2.63
1.8 | 2.19 | 2.22
2.4 | 2.32 | 2.32

## Slide 70: Estimation of Modular Ratio of Reinforced Beds

## Slide 71: Two-Layered Soils
p
/ Unit area
r
Layer 1 E1
ν1
1
h
Perfectly adhesive interface
t
Layer 2
E2
z
•
a

## Slide 72: Normalized Stresses at Interface h/a = 1.0 (Fox 1948)

## Slide 73: Settlement Influence Factors for n1/n2 (a) 0.2/0.4; (b) 0.5/0.5 and © 0.35/0.35

## Slide 74: Normalized Vertical Stress Profiles – Homogeneous Ground, h/a = 0.2, 0.75 & 1.0
Chart: r/a
| -3 | -2.5 | -2 | -1.7500000000000011 | -1.5 | -1.25 | -1 | -0.75000000000000144 | -0.62500000000000144 | -0.5 | -0.35000000000000031 | -0.2 | -0.1 | 0.1 | 0.2 | 0.35000000000000031 | 0.5 | 0.62500000000000144 | 0.75000000000000144 | 1 | 1.25 | 1.5 | 1.7500000000000011 | 2 | 2.5 | 3
0.2 | 0.01 | 0.05 | 0.09 | 0.45 | 0.8 | 14.4 | 46.78 | 85 | 91.01 | 94.83 | 97.78 | 99.13 | 99.19 | 99.19 | 99.13 | 97.78 | 94.83 | 91.01 | 85 | 46.78 | 14.4 | 0.8 | 0.45 | 0.09 | 0.05 | 0.01
0.75 | 1.16 | 1.67 | 2.92 | 5.01 | 8.98 | 20.27 | 37.44 | 59.84 | 65.31 | 68.93 | 72.22 | 74.49 | 74.96 | 74.96 | 74.49 | 72.22 | 68.93 | 65.31 | 59.84 | 37.44 | 20.27 | 8.98 | 5.01 | 2.92 | 1.67 | 1.16
1 | 0.6 | 2.4 | 4.2 | 8.45 | 12.7 | 22.95 | 33.2 | 45.675 | 51.3625 | 55.8 | 60.15 | 63.3 | 63.95 | 63.95 | 63.3 | 60.15 | 55.8 | 51.3625 | 45.675 | 33.2 | 22.95 | 12.7 | 8.45 | 4.2 | 2.4 | 0.6
1.25 | 1 | 2.9875 | 4.975 | 7.7 | 12.675 | 21.2375 | 29.8 | 40.075 | 44.645 | 48.3 | 51.925 | 54.625 | 55.0875 | 55.0875 | 54.625 | 51.925 | 48.3 | 44.645 | 40.075 | 29.8 | 21.2375 | 12.675 | 7.7 | 4.975 | 2.9875 | 1
2 | 2.2 | 4.75 | 7.3 | 9.95 | 12.6 | 16.1 | 19.6 | 22.99 | 24.5 | 25.8 | 27.25 | 27.98 | 28.5 | 28.5 | 27.98 | 27.25 | 25.8 | 24.5 | 22.99 | 19.6 | 16.1 | 12.6 | 9.95 | 7.3 | 4.75 | 2.2
Chart: r/a
| -4 | -3 | -2.5 | -2 | -1.75 | -1.5 | -1.25 | -1 | -0.75000000000000155 | -0.62500000000000155 | -0.5 | -0.35000000000000031 | -0.2 | -0.1 | 0 | 0.1 | 0.2 | 0.35000000000000031 | 0.5 | 0.62500000000000155 | 0.75000000000000155 | 1 | 1.25 | 1.5 | 1.75 | 2 | 2.5 | 3 | 4
2 | 0.55 | 0.75 | 0.87 | 2.52 | 7.02 | 13.55 | 22.52 | 32.75 | 44.54 | 48.15 | 51.45 | 54.18 | 55.52 | 56.07 | 56.25 | 56.07 | 55.52 | 54.18 | 51.45 | 48.15 | 44.54 | 32.75 | 22.52 | 13.55 | 7.02 | 2.52 | 0.87 | 0.75 | 0.55
3 | 0.85 | 1.46 | 1.9 | 3.14 | 4.75 | 8.65 | 15.59 | 25.55 | 35.75 | 41.25 | 44.55 | 47.25 | 48.57 | 49.15 | 49.39 | 49.15 | 48.57 | 47.25 | 44.55 | 41.25 | 35.75 | 25.55 | 15.59 | 8.65 | 4.75 | 3.141 | 1.901 | 1.456 | 0.85
6 | 1.85 | 2.16 | 3.02 | 4.12 | 5.45 | 6.25 | 9.82 | 15.35 | 25.45 | 30.25 | 34.25 | 37.05 | 38.55 | 39.05 | 39.22 | 39.05 | 38.55 | 37.05 | 34.25 | 30.25 | 25.45 | 15.35 | 9.82 | 6.25 | 5.45 | 4.12 | 3.02 | 2.158 | 1.85
10 | 2.12 | 1.24 | 2.02 | 3.12 | 3.75 | 5.02 | 7.52 | 12.24 | 18.45 | 20.75 | 22.45 | 23.85 | 24.55 | 25.02 | 25.18 | 25.02 | 24.55 | 23.85 | 22.45 | 20.75 | 18.45 | 12.24 | 7.52 | 5.02 | 3.75 | 3.12 | 2.02 | 1.24 | 2.12
20 | 2.22 | 0.86 | 1.19 | 2.15 | 3.55 | 4.75 | 6.22 | 8.15 | 10.52 | 11.55 | 12.86 | 14.52 | 15.95 | 16.58 | 16.85 | 16.58 | 15.95 | 14.52 | 12.86 | 11.55 | 10.52 | 8.15 | 6.22 | 4.75 | 3.55 | 2.15 | 1.19 | 0.86 | 2.22
Chart: r/a
| -4 | -3 | -2.5 | -2 | -1.75 | -1.5 | -1.25 | -1 | -0.75000000000000155 | -0.62500000000000155 | -0.5 | -0.35000000000000031 | -0.2 | -0.1 | 0 | 0.1 | 0.2 | 0.35000000000000031 | 0.5 | 0.62500000000000155 | 0.75000000000000155 | 1 | 1.25 | 1.5 | 1.75 | 2 | 2.5 | 3 | 4
2 | 0.75 | 0.99 | 2.42 | 5.68 | 8.03 | 12.42 | 22.52 | 34.01 | 43.21 | 46.42 | 49.52 | 51.73 | 53.15 | 53.63 | 53.86 | 53.63 | 53.15 | 51.73 | 49.52 | 46.42 | 43.21 | 34.01 | 22.52 | 12.42 | 8.028 | 5.675 | 2.42 | 0.9878 | 0.75
3 | 0.86 | 1.46 | 3.6 | 6.84 | 9.18 | 12.62 | 18.56 | 26.26 | 34.22 | 37.69 | 40.92 | 44.15 | 46.42 | 47.09 | 47.45 | 47.09 | 46.42 | 44.15 | 40.92 | 37.69 | 34.22 | 26.26 | 18.56 | 12.62 | 9.178 | 6.841 | 3.601 | 1.456 | 0.86
6 | 1.58 | 2.16 | 4.22 | 7.11 | 9.42 | 12.32 | 16.58 | 20.62 | 25.13 | 27.49 | 29.97 | 32.79 | 34.92 | 35.96 | 36.32 | 35.96 | 34.92 | 32.79 | 29.97 | 27.49 | 25.129 | 20.621 | 16.583 | 12.32 | 9.42 | 7.112 | 4.22 | 2.158 | 1.58
10 | 1.46 | 2.2 | 3.35 | 5.49 | 6.89 | 8.67 | 11.02 | 13.25 | 15.45 | 16.52 | 17.59 | 19.15 | 20.25 | 21.03 | 21.24 | 21.03 | 20.25 | 19.15 | 17.59 | 16.52 | 15.45 | 13.25 | 11.02 | 8.67 | 6.89 | 5.49 | 3.35 | 2.2 | 1.46
20 | 0.42 | 1.75 | 2.46 | 3.2 | 4.02 | 5.01 | 6.41 | 7.75 | 9.25 | 9.86 | 10.99 | 12.05 | 13.15 | 13.85 | 14.1 | 13.85 | 13.15 | 12.05 | 10.99 | 9.86 | 9.25 | 7.75 | 6.41 | 5.01 | 4.02 | 3.2 | 2.46 | 1.75 | 0.42
Chart: r/a
| -3 | -2.5 | -2 | -1.75 | -1.5 | -1.25 | -1 | -0.750000000000003 | -0.625000000000003 | -0.5 | -0.35000000000000031 | -0.2 | -0.1 | 0 | 0.1 | 0.2 | 0.35000000000000031 | 0.5 | 0.625000000000003 | 0.750000000000003 | 1 | 1.25 | 1.5 | 1.75 | 2 | 2.5 | 3
E1/E2=2 | 0.172 | 0.212 | 1.21 | 2.24 | 7.01 | 17.34 | 28.19 | 38.46 | 41.55 | 44.25 | 46.25 | 47.43 | 48.15 | 48.25 | 48.15 | 47.43 | 46.25 | 44.25 | 41.55 | 38.46 | 28.19 | 17.34 | 7.01 | 2.24 | 1.21 | 0.212 | 0.172
E1/E2=3 | 0.57 | 0.64 | 0.96 | 1.69 | 4.17 | 9.31 | 18.85 | 30.02 | 34.25 | 37.12 | 39.69 | 41.25 | 41.7 | 41.75 | 41.7 | 41.25 | 39.69 | 37.12 | 34.25 | 30.02 | 18.85 | 9.31 | 4.17 | 1.69 | 0.96 | 0.64 | 0.57
E1/E2=6 | 0.95 | 0.87 | 0.75 | 0.93 | 1.82 | 4.25 | 11.75 | 20.1 | 24.7 | 28.12 | 31.1 | 32.82 | 33.36 | 33.45 | 33.36 | 32.82 | 31.1 | 28.12 | 24.7 | 20.1 | 11.75 | 4.25 | 1.82 | 0.93 | 0.75 | 0.87 | 0.95
E1/E2=10 | 1.86 | 1.56 | 1.42 | 1.22 | 1.01 | 2.28 | 5.12 | 9.44 | 12.1 | 14.22 | 16.85 | 18.53 | 19.28 | 19.52 | 19.28 | 18.53 | 16.85 | 14.22 | 12.1 | 9.44 | 5.12 | 2.28 | 1.01 | 1.22 | 1.42 | 1.56 | 1.86
E1/E2=20 | 1.22 | 1.42 | 1.55 | 2.02 | 2.08 | 2.4 | 3.22 | 5.75 | 7.2 | 8.55 | 10.18 | 11.55 | 12.27 | 12.55 | 12.27 | 11.55 | 10.18 | 8.55 | 7.2 | 5.75 | 3.22 | 2.4 | 2.08 | 2.02 | 1.55 | 1.42 | 1.22

## Slide 75: Normalized Vertical Stress Profiles at Interface h/a =1.25 & 2.0
Chart: r/a
| -4 | -3 | -2.5 | -2 | -1.75 | -1.5 | -1.25 | -1 | -0.75000000000000144 | -0.62500000000000144 | -0.5 | -0.35000000000000031 | -0.2 | -0.1 | 0 | 0.1 | 0.2 | 0.35000000000000031 | 0.5 | 0.62500000000000144 | 0.75000000000000144 | 1 | 1.25 | 1.5 | 1.75 | 2 | 2.5 | 3 | 4
2 | 0.65 | 0.97 | 1.08 | 1.52 | 5.07 | 10.52 | 18.52 | 25.52 | 33 | 36.4 | 39.91 | 42.49 | 43.75 | 44.12 | 44.38 | 44.12 | 43.75 | 42.49 | 39.91 | 36.4 | 33 | 25.52 | 18.52 | 10.52 | 5.069 | 1.515 | 1.08 | 0.97 | 0.65
3 | 0.55 | 0.87 | 1.14 | 1.88 | 4.25 | 7.98 | 13.57 | 20.19 | 27.08 | 30.86 | 34.36 | 37.05 | 38.74 | 39.48 | 39.76 | 39.48 | 38.74 | 37.05 | 34.36 | 30.86 | 27.08 | 20.19 | 13.573 | 7.98 | 4.25 | 1.882 | 1.1431 | 0.87 | 0.55
6 | 0.85 | 1.77 | 2.48 | 3.13 | 4.05 | 6.05 | 9.35 | 14.58 | 20.88 | 24.18 | 26.45 | 28.33 | 29.55 | 30.22 | 30.33 | 30.22 | 29.55 | 28.33 | 26.45 | 24.18 | 20.88 | 14.5837 | 9.3489 | 6.05 | 4.0537 | 3.126 | 2.481 | 1.77 | 0.85
10 | 1.02 | 1.45 | 2.02 | 2.55 | 3.56 | 4.75 | 6.52 | 9.22 | 12.12 | 13.45 | 14.55 | 15.35 | 15.95 | 16.15 | 16.35 | 16.15 | 15.95 | 15.35 | 14.55 | 13.45 | 12.12 | 9.22 | 6.52 | 4.75 | 3.56 | 2.55 | 2.02 | 1.45 | 1.02
20 | 0.42 | 0.11 | 0.21 | 0.33 | 0.55 | 1.25 | 2.35 | 3.65 | 5.15 | 5.95 | 6.85 | 7.85 | 8.75 | 9.02 | 9.25 | 9.02 | 8.75 | 7.85 | 6.85 | 5.95 | 5.15 | 3.65 | 2.35 | 1.25 | 0.55 | 0.33 | 0.21 | 0.11 | 0.42
Chart: r/a
| -4 | -3 | -2.5 | -2 | -1.75 | -1.5 | -1.25 | -1 | -0.75000000000000144 | -0.62500000000000144 | -0.5 | -0.35000000000000031 | -0.2 | -0.1 | 0 | 0.1 | 0.2 | 0.35000000000000031 | 0.5 | 0.62500000000000144 | 0.75000000000000144 | 1 | 1.25 | 1.5 | 1.75 | 2 | 2.5 | 3 | 4
2 | 0.65 | 0.85 | 1.15 | 2.12 | 9.03 | 17.45 | 25.26 | 30.25 | 33.55 | 34.65 | 35.82 | 36.55 | 36.85 | 37.02 | 37.12 | 37.02 | 36.85 | 36.55 | 35.82 | 34.65 | 33.55 | 30.25 | 25.26 | 17.45 | 9.028 | 2.12 | 1.15 | 0.85 | 0.65
3 | 0.9 | 1.46 | 2.12 | 3.12 | 4.52 | 9.52 | 14.55 | 20.12 | 23.77 | 25.35 | 26.65 | 27.85 | 28.65 | 28.95 | 29 | 28.95 | 28.65 | 27.85 | 26.65 | 25.35 | 23.77 | 20.12 | 14.55 | 9.52 | 4.52 | 3.12 | 2.12 | 1.456 | 0.85
6 | 0.88 | 2.16 | 2.65 | 3.22 | 4.15 | 6.55 | 9.55 | 12.52 | 15.65 | 16.75 | 17.95 | 18.95 | 19.65 | 20.02 | 20.05 | 20.02 | 19.65 | 18.95 | 17.95 | 16.75 | 15.65 | 12.52 | 9.55 | 6.55 | 4.15 | 3.22 | 2.65 | 2.158 | 0.88
10 | 0.55 | 0.75 | 1.08 | 2.12 | 2.75 | 3.55 | 4.85 | 6.25 | 7.95 | 8.75 | 9.86 | 10.85 | 11.52 | 11.95 | 12.01 | 11.95 | 11.52 | 10.85 | 9.86 | 8.75 | 7.95 | 6.25 | 4.85 | 3.55 | 2.75 | 2.12 | 1.08 | 0.75 | 0.55
20 | 0.22 | 0.55 | 0.75 | 0.95 | 1.22 | 1.55 | 2.02 | 2.82 | 3.75 | 4.22 | 4.85 | 5.52 | 5.95 | 6.15 | 6.35 | 6.15 | 5.95 | 5.52 | 4.85 | 4.22 | 3.75 | 2.82 | 2.02 | 1.55 | 1.22 | 0.95 | 0.75 | 0.55 | 0.22

## Slide 76: Fitting Bell Curve

## Slide 77: Integration for Partial Load
= Pa/P0

## Slide 78: Radial Extent vs h/a
Chart: h/a
| F0.98 | 1.298602 | 1.8917 | 1.9749 | 98 | 16.6 | 41.7 | 44.3 | F0.95 | 1.23229 | 1.768 | 1.8745 | 95 | 13.1 | 37.5 | 41.2 | F0.9 | 1.1441 | 1.60506 | 1.7242 | 90 | 8.2 | 31.2 | 35.9 | F0.85 | 1.0707 | 1.4393 | 1.5745 | 85 | 4 | 23.7 | 29.9 | r/a | F0.8 | 1.0023 | 1.3163 | 1.4742 | Spread Angle | 80 | 0.1 | 17.6 | 25.4
Fz= Fz/Fo=
0 0
Integration 0.402
Integration 0.402
Integration 0.402
Integration 0.402
Integration 0.402
Integration 0.402
Integration 0.402
Fz= Fz/Fo= | 1.0023 | 1.161 | 1.3163 | 1.4742 | 1.78 | 2.2
0 0 | 1.0707 | 1.25 | 1.3993 | 1.5745 | 1.93 | 2.375
Integration 0.402 | 1.1441 | 1.35 | 1.522 | 1.7242 | 2.1 | 2.57

## Slide 79: h/a = 0.2, 0.75, 1.0 & 1.25
Chart: R vs. E1/E2
| 2 | 3 | 6 | 10 | 20
 | 1.4803 | 1.544 | 1.739 | 1.99 | 2.67
 | 1.4023 | 1.46 | 1.65 | 1.88 | 2.4
 | 1.3341 | 1.4 | 1.5666 | 1.75 | 2.21
 | 1.29 | 1.34 | 1.49 | 1.65 | 2.022
Chart: E1/E2
| 2 | 3 | 6 | 10 | 20
 | 2.11 | 2.25 | 2.61 | 3.02 | 4.12
 | 1.95 | 2.08 | 2.42 | 2.77 | 3.74
 | 1.84 | 1.95 | 2.25 | 2.59 | 3.42
 | 1.75 | 1.83 | 2.09 | 2.38 | 3.12

Chart: Rvs. E1/E2
| 2 | 3 | 6 | 10 | 20
 | 2.06 | 2.17 | 2.62 | 3.21 | 4.56
 | 1.95 | 2.06 | 2.49 | 2.99 | 4.22
 | 1.89 | 1.99 | 2.34 | 2.82 | 3.86
 | 1.828 | 1.92 | 2.22 | 2.66 | 3.55

Chart: R vs. E1/E2
| 2 | 3 | 6 | 10 | 20
 | 2.2142 | 2.312 | 2.693 | 3.33 | 5.14
 | 2.098 | 2.187 | 2.52 | 3.05 | 4.65
 | 2.022 | 2.11 | 2.39 | 2.91 | 4.22
 | 1.943 | 2.02 | 2.32 | 2.75 | 3.85


## Slide 80: h/a = 2.0
Chart: R vs. E1/E2
| 2 | 3 | 6 | 10 | 20
 | 2.677 | 2.74 | 3.12 | 3.66 | 5.42
 | 2.546 | 2.62 | 2.92 | 3.44 | 5.01
 | 2.421 | 2.48 | 2.75 | 3.22 | 4.55
 | 2.288 | 2.32 | 2.54 | 2.92 | 4.05


## Slide 81: Effect of Modular ratio
Chart: m
| 2 | 3 | 6 | 10 | 20
0.2 | 1.29 | 1.34 | 1.49 | 1.65 | 2.022
0.75+Sheet3!$H$6:$H$10 | 1.75 | 1.83 | 2.09 | 2.38 | 3.12
1 | 1.828 | 1.92 | 2.22 | 2.66 | 3.55
1.25 | 1.943 | 2.02 | 2.32 | 2.75 | 3.85
2 | 2.288 | 2.32 | 2.54 | 2.92 | 4.05
Chart: m
| 2 | 3 | 6 | 10 | 20
0.2 | 1.3341 | 1.4 | 1.5666 | 1.75 | 2.21
0.75 | 1.84 | 1.95 | 2.25 | 2.59 | 3.42
1 | 1.89 | 1.99 | 2.34 | 2.82 | 3.86
1.25 | 2.022 | 2.11 | 2.39 | 2.91 | 4.22
2 | 2.421 | 2.48 | 2.75 | 3.22 | 4.55
Chart: m
| 2 | 3 | 6 | 10 | 20
0.2 | 1.4023 | 1.46 | 1.65 | 1.88 | 2.4
0.75 | 1.95 | 2.08 | 2.42 | 2.77 | 3.74
1 | 1.95 | 2.06 | 2.49 | 2.99 | 4.22
1.25 | 2.098 | 2.187 | 2.52 | 3.05 | 4.65
2 | 2.546 | 2.62 | 2.92 | 3.44 | 5.01

## Slide 82: Case study 1- (Murad et al., 2008).
Reinforcement | Tensile modulus(kN/m)
GG1 | 182
GG2 | 274
GG3 | 425

## Slide 83
(a) 457 mm
(b) 610 mm
Measured vertical stress distributions at depth (Murad et al., 2008).

## Slide 84: Measured vertical stress distributions at depth of 762 mm (Murad et al., 2008).
(c) 762 mm

## Slide 85
Schematic a)Reinforced soil bed and
b)Two-layered system for h = 457 mm
(a)
(b)
E1 , ν1
E2 , ν2
Reinforcement layer 1
2
Pressure cells

## Slide 86: Schematic a)Reinforced soil bed and b)Two-layered system for h = 610 mm
(a)
(b)
E1 , ν1
E2 , ν2
Reinforcement layer 1
2
3
Pressure cells

## Slide 87
(a)
(b)
Schematic - a)Reinforced soil bed and
b) Two layered system for h = 762 mm.
E1 , ν1
E2 , ν2
Reinforcement layer 1
2
3
4
Pressure cells

## Slide 88: Load distribution angle (θ) vs  (Murad et al., 2008)
Chart: 
| 75 | 80 | 85 | 90 | 95
GG14 | 46.4 | 50.8 | 54.8 | 58.8 | 63.7
GG23 | 45 | 49.6 | 53.5 | 58 | 63.1
GG24 | 47.7 | 51.9 | 55.9 | 59.9 | 64.3
GG25 | 52.4 | 56.3 | 59.9 | 63.1 | 67.2
GG34 | 49 | 52.4 | 56.3 | 60.3 | 64.8
E1/E2=1 | 1.975 | 2.125 | 2.325 | 2.575 | 2.9
Chart: 
| 75 | 80 | 85 | 90 | 95
GG14 | 61.9 | 64.8 | 67.2 | 69.8 | 72.5
GG23 | 61.3 | 63.7 | 66.3 | 69.1 | 72.3
GG24 | 62.9 | 65.6 | 68 | 70.5 | 73.3
GG25 | 64 | 66.3 | 68.8 | 71.1 | 73.9
GG34 | 62.9 | 65.3 | 67.8 | 70.2 | 73
h/a = 2.0 h/a = 2.66

## Slide 89: (θ) vs  for h/a = 3.34 (Murad et al., 2008)
Chart: 
| 75 | 80 | 85 | 90 | 95
GG14 | 65.3 | 67.6 | 69.8 | 72.1 | 74.7
GG23 | 65.6 | 67.8 | 70 | 72.5 | 74.7
GG24 | 66.7 | 68.8 | 70.8 | 72.8 | 75.2
GG25 | 69.1 | 71.1 | 72.8 | 74.6 | 76.5
GG34 | 67.6 | 69.5 | 71.4 | 73.5 | 75.6

## Slide 90: Interpolation for modular ratio for 90% load (Murad et al., 2008)

## Slide 91: Modular ratios for RFB: thickness 457 mm, h/a = 2.0
h/a=2.0 | Reinforcement | µ
 | GG14 | 3.9
 | GG23 | 3.8
 | GG24 | 4.4
 | GG25 | 6.1
 | GG34 | 5.4
Average for geogrids |  | 4.7

## Slide 92: Modular ratios for RFB: thickness 610 mm, h/a = 2.66
h/a = 2.66 | Reinforcement | μ
 | GG14 | 8.9
 | GG23 | 8.2
 | GG24 | 9.4
 | GG25 | 10.2
 | GG34 | 9.6
 | Average for geogrids | 9.3

## Slide 93: Modular ratios for RFB: Thickness 762 mm, h/a = 3.34
h/a = 3.34 | Reinforcement | μ
 | GG14 | 9.6
 | GG23 | 9.5
 | GG24 | 10.3
 | GG25 | 12.0
 | GG34 | 11.1
Average for geogrids |  | 10.5

## Slide 94: Case study 2 - (Chen et al., 2007)
Reinforcement | Tensile modulus(kN/m)
GG1 | 365
GG2 | 182
GG3 | 274
GT1 | 700

## Slide 95: Stress distributions: depth of 254 mm Surface pressure (a) 47 kPa and (b) 468 kPa, (Chen et al., 2007)
(a)
(b)

## Slide 96: Schematic – h = 254 mm
(a)
(b)
E1 , ν1
E2 , ν2
h = 254
mm

## Slide 97: (θ) vs  (Chen et al., 2007)
Chart: 
| 80 | 85 | 90 | 95
80 | 68 | 70.5 | 72.7 | 73.1
85 | 68.4 | 70.8 | 72.9 | 73.3
90 | 63.7 | 67.1 | 70.1 | 71.8
95 | 71.1 | 72.3 | 73.2 | 73.7

## Slide 98
h/a = 3.34 | Reinforcement | μ
 | GG1 | 10.2
 | GG2 | 10.4
 | GG3 | 8.1
 | Average for geogrids | 9.6
 | GT1 | 10.7
Modular ratios for RFB:
Thickness 254 mm, h/a = 3.34 (Chen et al., 2007)

## Slide 99: Case study 3 (Murad et al, 2013).
Reinforcement | Tensile modulus (kN/m)
GG1 | 365
GT1 | 700

## Slide 100: Stress distribution at depth of 254 mm for surface pressure (a) 94 kPa and (b) 750 kPa, (Murad et al, 2013)

## Slide 101
(a)
(b)
Schematic
E1 , ν1
E2 , ν2
h= 254
mm

## Slide 102: (θ) vs  (Murad et al, 2013)
Chart: 
| 80 | 85 | 90 | 95
GG1 | 71.3 | 72.8 | 73.7 | 74.2
GT1 | 72.7 | 74 | 74.8 | 75.2

## Slide 103: Modular ratios for RFB Thickness 254 mm, h/a = 3.34 (Murad et al, 2013)
h/a = 3.34 | Reinforcement | µ
 | GG1 | 11.2
 | GT1 | 12.4
Average for reinforcement |  | 11.8

## Slide 104: Moral – Do Not Prescribe Pile Foundations unless Essential. Think of The Third Alternative - GRGB

## Slide 105: There is Life in the Ground: it goes into the seed and it also, when stirred up, goes into the man who stirs it. C. D. Warner
13/05/2026
105